# PART 1 GENERAL

  - SECTION INCLUDES

- Fabricated sheet metal items, including flashings, counterflashings, gutters, and downspouts.

- Reglets and accessories.

  - RELATED REQUIREMENTS

- Section 099100 – Joint Sealers.

  - REFERNCE STANDARDS

- AAMA 2605 – Voluntary Specification, Performance Requirements and Test Procedures for Superior Performing Organic Coatings on Aluminum Extrusions and Panels; 2005.

- ASTM A 653/A 653M – Standard Specifications for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process; 2007.

- SMACNA (ASMM) – Architectural Sheet Metal Manual; Sheet Metal and Air Conditioning Contractors’ National Association; 2003.

  - Submittals

- See Section 01300 – Administrative Requirements, for submittal procedures.

- Shop Drawings: Indicate material profile, jointing pattern, jointing details, fastening methods, flashings, terminations, and installation details.

  - QUALITY ASSURANCE

- Perform work in accordance with SMACNA Architectural Sheet Metal Manual requirements and standard details, except as otherwise indicated.

- Fabricator and Installer Qualifications: Company specializing in sheet metal work with 5 years of documented experience.

  - DELIVERY, STORAGE AND HANDLING

  - Stack material to prevent twisting, bending, abrasion and to provide ventilation.  Slope metal sheets to ensure drainage.

  - Prevent contact with materials that could cause discoloration or staining.

# PART 2 PRODUCTS

  - SHEET MATERIALS

- Pre-Finished Galvanized Steel: ASTM A 653/A 653M, with G90/Z275 zinc coating; minimum 0.02 inch thick base metal, shop pre-coated with PVDF coating.

  - PVDF (Polyvinylidene Flouride) Coating: Superior Performance Organic Finish, AAMA 2605; multiple coat, thermally cured fluoropolymer finish system; color as selected from the manufacturer’s standard colors.

  - ACCESSORIES

- Fasteners: Galvanized steel, with soft neoprene washers. Color to match adjacent material.

- Underlayment: Grace Building Products, Grace Ice and WaterShield.

- Primer: Zinc chromate type.

- Protective Backing Paint: Zinc molybdate alkyd.

  - FABRICATION

- Form section true to shape, accurate in size, square, and free from distortion or defects.

- Form pieces in longest possible lengths.

- Hem exposed edges on underside 1/2 inch; miter and seam corners.

- Form material with standing seam, except where otherwise indicated.  At moving joints, use seal lapped bayonet-type or interlocking hooked seams.

- Provide standing seam joint at all coping joints.

- Fabricate corners from one piece with minimum 18 inch long legs; seam for rigidity, seal with sealant.

- Fabricate vertical faces with bottom edge formed outward 1/4 inch and hemmed to form drip.

# PART 3 EXECUTION

3.01	EXAMINATION

- Verify roof openings, curbs, pipes, sleeves, ducts, and vents through roof are solidly set, reglets in place and nailing strips located.

- Verify roofing termination and base flashings are in place, sealed and secure.

  - PREPARATION

  - Coordinate installation with installation of metal wall panels and sheathing membrane.

  - Install starter and edge strips, and cleats before starting installation.

  - Install surface mounted reglets true to lines and levels.  Seal top of reglets with sealant.

  - Back paint concealed metal surfaces with protective backing paint to a minimum dry film thickness of 15 mil.

  - INSTALLATION

- Conform to drawing details and applicable SMACNA details.

- Secure flashings in place using concealed fasteners.  Use exposed fasteners only where permitted.

- Apply plastic cement compound between metal flashings and felt flashings.

- Fit flashings tight in place.  Make corners square, surfaces true and straight in planes, and lines accurate to profiles.

# End of Section 07 62 00