PART 1 - GENERAL

  - SECTION INCLUDES

- Standard insulated hollow metal doors and frames

  - RELATED SECTION

- Section 087100 - Door Hardware

- Section 099000 - Paints and Coatings

  - RELATED DOCUMENTS

- Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specifications Sections, apply to this Section.

  - DEFINITIONS

- Minimum Thickness: Minimum thickness of base metal without coatings, 22 Gauge.

- Standard Hollow Metal Work: Hollow metal work fabricated according to ANSI/SDI A250.8.

  - SUBMITTALS

- Product Data: For each type of product indicated. Include construction details, material descriptions, core descriptions, fire-resistance rating, temperature-rise ratings, and finishes.

- Shop Drawings: Include the following:

- Elevations of each door design

- Details of doors, including vertical and horizontal edge details and metal thicknesses.

- Frame details for each frame type, including dimensioned profiles and metal thicknesses.

- Locations of reinforcement and preparations for hardware.

- Details of each different wall opening condition.

- Details of anchorages, joints, field splices, and connections.

- Details of accessories.

- Details of moldings, removable stops, and glazing.

- Samples for Initial Selection: For units with factory-applied color finishes.

- Samples for Verification:

- For each type of exposed finish required, prepared on Samples of not less than 3 by 5 inches (75 by 125 mm.)

- For the following items, prepared on Samples about 12 by 12 inches (305 by 305 mm) to demonstrate compliance with requirements for quality of materials and construction:

  - Doors: Show vertical-edge, top, and bottom construction; core construction; and hinge and other applied hardware reinforcement. Include separate section showing glazing if applicable.

  - Frames: Show profile, corner joint, floow and wall anchors, and silencers. Include separate section showing fized hollow metal panels and glazing if applicable.

- Other Action Submittals:

- Schedule: Provide a schedule of hollow metal work prepared by or under the supervision of supplier, using same reference numbers for details and openings as those on Drawings. Coordinate with door hardware schedule.

- Product Test Reports: Based on evaluation of comprehensive tests performed by a qualified testing agency, for each type of hollow metal door and frame assembly.

  - QUALITY ASSURANCE

- Source Limitations: Obtain hollow metal work from single source from single manufacturer.

  - DELIVERY, STORAGE, AND HANDLING

- Deliver hollow metal work palletized, wrapped, or crated to provide protection during transit and Project-site storage. Do not use non-vented plastic.

- Provide additional protection to prevent damage to finish of factory-finished units.

- Deliver welded frames with two removable spreader bars across bottom of frames, tack welded to jambs and mullions.

- Store hollow metal work under cover at Project site. Place in stacks of five units maximum in a vertical position with heads up, spaced by blocking, on minimum 4-inch high wood blocking. Do not store in a matter than traps excess humidity.

- Provide minimum ¼-inch space between each stacked door to permit air circulation.

  - PROJECT CONDITIONS

- Field Measurements: Verify actual dimensions of openings by field measurements before fabrication.

  - COORDINATION

- Coordinate installation of anchorages for hollow metal frames. Furnish setting drawings, templates, and directions for installing anchorages, including sleeves, concrete inserts, anchor bolts, and items with integral anchors. Deliver such items to Project site in time for installation.

PART 2 - PRODUCTS

  - MANUFACTURERS

- Manufacturers: Subject to compliance with requirements, provide products by one of the following.

- Lyndon or Equivalent

  - MATERIALS

- Cold-Rolled Steel Sheet: ASTM A 1008/A 1008 M, Commercial Steel (CS), Type B; suitable for exposed applications.

- Metallic-Coated Steel Sheet: ASTM A 653/A 653M, Commercial Steel (CS), Type B; with minimum A60 (ZF180) metallic coating.

- Frame Anchors: ASTM A 591/A 591M, Commercial Steel (CS), 40Z (12G) coating designation; mill phosphatized.

- For anchors built into exterior walls, steel sheet complying with ASTM A 1008/A 1008M or ASTM A 1011/A 1011M, hot-dip galvanized according to ASTM A 153/A 153M, Class B.

- Inserts, Bolts, and Fasteners: Hot-dip galvanized according to ASTM A 153/A 153M.

- Bituminous Coating: Cold-applied asphalt mastic, SSPC-Paint 12, compounded for 15-mil (0.4-mm) dry film thickness per coat. Provide inert-type noncorrosive compound free of asbestos fibers, sulfur components, and other deleterious impurities.

  - STANDARD HOLLOW METAL DOORS

- General: Provide doors of design indicated, not less than thickness indicated; fabricated with smooth surfaces, without visible joints or seams on exposed faces unless otherwise indicated. Comply with ANSI/SDI A250.8.

- Design: As indicated on door schedule.

- Core Construction: Polystyrene, polyurethane, mineral-board, or vertical steel-stiffener core.

- Vertical Edges: Seamless, continuously welded, ground smooth with no putty, no filler.

- Top and Bottom Edges: Closed with flush or inverted 0.053-inch- (1.3-mm-) thick, end closures or channels of same material as face sheets.

- Tolerances: Comply with SDI 117, “Manufacturing Tolerances for Standard Steel Doors and Frames.”

- Exterior Doors: Face sheets fabricated fro metallic-coated steel sheet. Provide doors complying with requirements indicated below by referencing ANSI/SDI A250.8 for level model and ANSI/SDI A250.4 for physical performance level:

- Level 2 and Physical Performance Level B (Heavy Duty), Model 2 - Seamless, continuously welded, ground smooth, no putty, no filler.

- Hardware Reinforcement: Fabricate according to ANSI/SDI A250.6 with reinforcing plates from same material as door face sheets.

- Fabricate concealed stiffeners and hardware reinforcement from either cold- or hot-rolled steel sheet.

  - STANDARD HOLLOW METAL FRAMES

- General: Comply with ANSI/SDI A250.8 and with details indicated for type and profile.

- Exterior Frames: Fabricated from metallic-coated steel sheet.

- Fabricate frames with mitered corners.

- Fabricate frames as full profile welded unless otherwise indicated.

- Frames for Level 2 Steel Doors: 0.053-inch- (1.3-mm-) thick steel sheet.

- Hardware Reinforcement: Fabricate according to ANSI/SDI A250.6 with reinforcement plates from same material as frames.

  - FRAME ANCHORS

- Floor Anchors: Formed from same material as frames, not less than 0.042 inch (1.0mm) thick, and as follows:

- Monolithic Concrete Slabs: Clip-type anchors, with two holes to receive fasteners.

- Separate Topping Concrete Slabs: Adjustable-type anchors with extension clips, allowing not less than 2-inch (50-mm) height adjustment. Terminate bottom of frames at finish floor surface.

  - HOLLOW METAL PANELS

- Provide hollow metal panels of same materials, construction, and finish as specified for adjoining hollow metal work.

  - STOPS AND MOLDINGS

- Provide stops and molding around glazed lites where indicated. Form corners of stops and moldings with butted or mitered hairline joints.

- Moldings for Glazed Lites in Doors: Provide fixed stops and moldings with no exposed fasteners on secure side of hollow metal work.

- Fixed Frame Moldings: Formed integral with hollow metal frames, a minimum of 5/8 inch (16 mm) high unless otherwise indicated. Use manufacturer’s standard glazing bead.

- Loose Stops for Glazed Lites in Frames: Minimum 5.8 inch (16 mm) high, fabricated from manufacturer’s standard glazing bead.

- Terminated Stops: Where indicated on interior door frames, terminate stops 6 inches (152mm) above finish floor with a 45-degree angle cut, and close open end of stop with steel sheet closure. Cover opening in extension of frame with welded-steel filler plate, with welds ground smooth and flush with frame.

- Provide terminated stops where indicated.

  - ACCESSORIES

- Mullions and Transom Bars: Join to adjacent members by welding or rigid mechanical anchors.

- Ceiling Struts: Minimum ¼-inch-thick by 1-inch- (6.4-mm-thick by 25.4-mm-) wide steel.

  - FABRICATION

- Fabricate hollow metal work to be rigid and free of defects, warp, or buckle. Accurately form metal to required sizes and profiles, with minimum radius for thickness of metal. Where practical, fit and assemble units in manufacturer’s plant. To ensure proper assembly at Project site, clearly indentify work that cannot be permanently factor assembled before shipment.

- Tolerances: Fabricate hollow metal work to tolerances indicated in SDI 117.

- Hollow Metal Frames: Where frames are fabricated in sections due to shipping or handling limitations, provide alignment plates or angles at each joint, fabricated of same thickness metal as frames.

- Welded Frames: Weld flush face joints continuously; grind, fill, dress, and make smooth, flush and invisible.

- Provide countersunk, flat- or oval-head exposed screws and bolts for exposed fasteners unless otherwise indicated.

- Floor Anchors: Weld anchors to bottom of jambs and mullions with at least four spot welds per anchor.

- Jamb Anchors: Provide number and spacing of anchors as follows:

- Stud-Wall Type: Locate anchors not more than 18 from top and bottom of frame. Space anchors not more than 32 inches O.C. and as follows:

    - Three anchors per jamb up to 60 inches high.

    - Four anchors per jamb from 60 to 90 inches high.

    - Five anchors per jamb from 90 to 96 inches high.

    - Five anchors per jamb plus (1) additional anchor per jamb for each 24 inches or fractions thereof above 96 inches high.

    - Two anchors per head for frames above 42 inches wide and mounted in metal-stud partitions.

- Compression Type: Not less than two anchors in each jamb.

- Post-installed Expansion Type: Locate anchors not more than (6) inches from top and bottom of frame. Space anchors not more than (26) inches O.C.

- Fabricate concealed stiffeners, edge channels, and hardware reinforcement from either cold- or hot-rolled steel sheet.

- Hardware Preparation: Factory prepare hollow metal work to receive templated mortised hardware; include cutouts, reinforcement, mortising, drilling, and tapping according to the Door Hardware Schedule and templates furnished as specified in Section 087100: Door Hardware

- Locate hardware as indicated, or if not indicated, according to ANSI/SDI A250.8.

- Reinforce doors and frames to receive nontemplated, mortised and surface-mounted door hardware.

- Comply with applicable requirements in ANSI/SDI A250.6 and ANSI/DHI A115 Series specifications for preparations of hollow metal work for hardware.

- Coordinate locations of conduit and wiring boxes for electrical connections with Division 26 Sections.

- Stops and Moldings: Provide stops and moldings around glazed lites where indicated. Form corners of stops and moldings with burred or mitered hairline joints.

- Single Glazed Lites: Provide fixed stops and moldings with no exposed fasteners on secure side of hollow metal work.

- Multiple Glazed Lites: Provide fixed and removable stops and moldings so that each glazed lite are capable of being removed independently.

- Provide fixed frame moldings on outside of exterior and on secure side of interior doors and frames.

- Provide loose stops and moldings on inside of hollow metal work.

- Coordinate rabbet width between fixed and removable stops with type of glazing and type of installation indicated.

  - STEEL FINISHES

- Prime Finish: Apply manufacturer’s standard primer immediately after cleaning and pretreating.

- Shop Primer: Manufacturer’s standard, fast-curing, lead- and chromate-free primer complying with ANSI/SDI A250.10 acceptance criteria; recommended by primer manufacturer for substrate; compatible with substrate and field-applied coatings despite prolonged exposure.

PART 3 - EXECUTION

  - EXAMINATION

- Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

- Examine roughing-in for embedded and built-in anchors to verify actual locations before frame installation.

- For the record, prepare written report, endorsed by Installer, listing conditions detrimental to performance of the Work.

- Proceed with installation only after unsatisfactory conditions have been corrected.

  - PREPARATION

- Remove welded-in shipping spreaders installed at factory. Restore exposed finish by grinding, filling, and dressing, as required to make repaired area smooth, flush, and invisible on exposed faces.

- Prior to installation, adjust and securely brace welded hollow metal frames for squareness, alignment, twist, and plumbness to the following tolerances.

- Squareness: Plus or minus 1/16inch, measured at door rabbet on a line 90 degrees from jamb perpendicular to frame head.

- Alignment: Plus or minus 1/16 inch, measured at jambs on horizontal line parallel to plane of wall.

- Twist: Plus or minus 1/16 inch, measured at opposite face corners of jambs on parallel lines, and perpendicular to plane of wall.

- Plumbness: Plus or minus 1/16 inch, measured at jambs on a perpendicular line from head to floor.

- Drill and tap doors ad frames to receive nontemplated, mortised, and surface-mounted door hardware.

  - INSTALLATION

- General: Install hollow metal work plumb, rigid, properly aligned, and securely fastened in place; comply with Drawings and manufacturer’s written instructions.

- Hollow Metal Frames: Install hollow metal frames of size and profile indicated. Comply with ANSI/SDI A250.11.

- Set frames accurately in position, plumbed, aligned, and braced securely until permanent anchors are set. After wall construction is complete, remove temporary braces, leaving surfaces smooth and undamaged.

- Where frames are fabricated in sections because of shipping or handling limitations, field splice at approved locations by welding face joint continuously; grind, fill, dress, and make splice smooth, flush, and invisible on exposed faces.

- Remove temporary braces necessary for installation only after frames have been properly set and secured.

- Check plumbness, squareness, and twist of frames as walls are constructed. Shim as necessary to comply with installation tolerances.

- Floor Anchors: Provide floor anchors for each jamb and mullion that extends to floor, and secure with post-installed expansion anchors.

- Floor anchors may be set with powder-actuated fasteners instead of post-installed expansion anchors if so indicated and approved on Shop Drawings.

- Installation Tolerances: Adjust hollow metal door frames for squareness, alignment, twist, and plumb to the following tolerances.

- Squareness: Plus or minus 1/16 inch, measured at door rabbet on a line 90 degrees from jamb perpendicular to frame head.

- Alignment: Plus or minus 1/16 inch, measured at jambs on a horizontal line parallel to plane of wall.

- Twist: Plus or minus 1/16 inch, measured at opposide face corners of jambs on parallel lines, and perpendicular to plane of wall.

- Plumbness: Plus or minus 1/16 inch, measured at jambs at floor.

- Hollow Metal Doors: Fit hollow metal doors accurately in frames, within clearances specified below. Shim as necessary.

- Non-Fire-Rated Standard Steel Doors:

- Jambs and Head: 1/8 inch plus or minus 1/16 inch.

- Between Edges of Pairs of Doors: 1/8 inch plus or minus 1/16 inch

- Between Bottom of Door and Top of Threshold: maximum 3/8 inch.

- Between Bottom of Door and Top of Finish Floor (No Threshold): Maximum 3/4 inch.

  - ADJUSTING AND CLEANING

- Final Adjustments: Check and readjust operating hardware items immediately before final inspection. Leave work in complete and proper operating condition. Remove and replace defective work, including hollow metal work that is warped, bowed, or otherwise unacceptable.

- Remove grout and other bonding material from hollow metal work immediately after installation

- Prime-Coat Touchup: Immediately after erection, sand smooth rusted or damaged areas of prime coat and apply touchup of compatible air-drying, rust-inhibitive primer.

- Metallic-Coated Surfaces: Clean abraded areas and repair with galvanizing repair paint according to manufacturer’s written instructions.

End of Section 08 11 13