PART 1  GENERAL

1.01	SECTION INCLUDES

A.	Hot Mix Asphalt.

1.02	RELATED SECTIONS

A.	Section 321100 – Base Courses

1.03	REFERENCES

A.	Washington State Department of Transportation (WSDOT) Standard Specifications for Road, Bridge, and Municipal Construction (current edition).

1.04	SUBMITTALS

A.	Product data and certification that asphalt concrete pavement materials comply with the specification requirements.  Include design mix formula and include laboratory test reports verifying compliance with the design mix formula.

B.	Product data and certification that tack materials comply with specification requirements.

1.05	QUALITY ASSURANCE

A.	Contractor shall have a minimum of five years of experience specializing in constructing asphalt roadways and must be willing to provide past performance references if requested by the Engineer.

B.	The Contractor will provide 3rd party compaction testing that conforms to Section 5-04.3(B)1 of the WSDOT Standard Specification to determine if asphalt has been properly consolidated.

PART 2  PRODUCTS

2.01	HOT MIX ASPHALT

- Hot mix asphalt concrete pavement shall be HMA Cl. ½” PG 64-22 and shall conform to Section 5-04.3 of the WSDOT Standard Specifications.

2.02	TACK

- Tack coat shall be required when new Asphalt Concrete Pavement is placed on, or abutting, existing asphalt.  Tack coat shall be CRS-1, as specified in Section 9-02.1(6) of the WSDOT Standard Specifications.

PART 3  EXECUTION

3.01	EXAMINATION

A.	Carefully investigate site condition and confirm that grading and placing of aggregate is to the correct elevation.  Contractor must maintain minimum thicknesses of pavement as called out on plans and shown in the details.

3.02	PREPARATION

A.	The surface of the top rock shall be approved by the Engineer prior to laying asphalt.

3.03	HOT-MIX ASPHALT

A.	Asphalt concrete pavement materials shall be placed on compacted subgrade materials, as shown on the Drawings, and in conformance with Sections 4-04, 4-06, and 5-04 of the WSDOT Standard Specifications.  The Contractor shall place asphalt concrete over prepared base course in a single lift.  Methods of proportioning, mixing, transporting, laying, processing, rolling, and compacting the material, and the standards of workmanship shall conform to the applicable requirements of Division  5 of the WSDOT Standard Specifications.

B.	HMA shall be compacted to 91% of the referenced maximum density as determined by WSDOT FOP for AASHTO T 209.

3.04	TACK

A.	All joints of asphalt concrete pavement shall be sealed with asphalt cement.  The asphalt paint binder, or tack coat, shall conform in all respects to Section 5-04 of the WSDOT Standard Specifications.  After pavement is in place, all joints shall be sealed with hot asphalt cement (CRS-1).

End of Section 32 12 16